## Slide 1
Question: Discuss how WMM is considered to be an improvement upon conventional WBM construction.
Or
Differentiate between WBM and WMM.
Criteria | WBM | WMM
 | Water Bound Macadam | Wet Mix Macadam
Use | Mostly used as Base Course, also may be used as sub-base or surfacing course depending upon category of road. | Mostly as Base Course for high traffic roads. Sometimes may be used as sub-base
Material | Coarse aggregates, Screening and binding material are applied separately. | Coarse aggregates: crushed stone/crushed gravel/ shingle, not less than 90% by weight of gravel/shingle pieces retained on 4.75 mm sieve. Aggregates are used in combined manner.

## Slide 2
Criteria | WBM | WMM
 | Water Bound Macadam | Wet Mix Macadam
Grading of Material | There are 3 gradings (G1: 90 mm to 45 mm, G2: 63 mm to 45 mm and G3: 53 mm to 22.4 mm) for Coarse aggregates and 2 gradings (13.2 mm and 11.2 mm screening size)for screenings. | There is only one grading requirement of aggregates for WMM from IS Sieve size 53 mm to 75 micron.
Compacted Thickness of each layer | For grading G1 is 100 mm and for grading G2 and G3 it is 75 mm. | Thickness of an individual layer shall not be less than 75 mm and can be up to 250 mm, for graded material.
Water Consumption | Copious use of water | Less consumption of water

## Slide 3
Criteria | WBM | WMM
 | Water Bound Macadam | Wet Mix Macadam
Construction | Corse aggregates are manually spread over the prepared surface. | The mix is prepared in the pugmill plant and then may be spread by a paver finisher and in case of multilayer construction the bottom layer/layers may be allowed to laid by motor grader
Compaction | After the laying of coarse aggregates rolling is done. After this screenings are applied to fill interstices followed by its rolling. Finally binding material is applied then its rolling is done. | Compaction of WMM mix is done in a single step, as mix is prepared.

## Slide 4
Criteria | WBM | WMM
Thickness of Compacted layer and type of roller used | It may be 100 mm or 75 mm depending upon grading of material. Three wheel-power roller of 80 to 100 kN capacity or an equivalent vibratory roller can be used. | It is up to 100 mm when smooth wheeled roller is used and up to 200 mm when vibratory wheeled roller is used.
Segregation Problem | Segregation takes place in mix and there is non-uniformity is the finished work | No segregation in mix. A dense uniform mass is obtained in the form of finished work
Time of construction | More time consuming as construction is done manually | Faster rate of construction as machinery is involved
Quality of Construction | Not very good | Good quality, because there is a good control over the mix, used in construction.
Cost | Cheaper than WMM | Costlier than WBM,